Guidance Notes and Specification for Road Openings

The applicant should contact all Statutory Undertakers for details of their apparatus before any excavations are carried out. Guidance should also be sought from North Ayrshire Council on the location of street lighting or traffic signal ducts.

All works must comply with the requirements of the Specification for the Reinstatement of Openings in Roads (October 2003 Edition), published by the Scottish Executive.

The reinstatement shall be to the compacted thicknesses as follows with each layer being fully compacted.  Where widths do not allow a twin drum or vibrating roller onto the material, it should be compacted by means of a vibrotamper.

All permanent reinstatements will be subject to a 12-month maintenance period, any defects which occur within the maintenance period shall be rectified at the applicant’s expense.

Flexible Carriageway (Permanent Reinstatement)

| Layer | Bus Routes/ Main Roads | Other Roads | Materials to be used |  |
| --- | --- | --- | --- | --- |
| Surface Course (a) | 40 mm | 40mm | Rolled Asphalt (CL 910) or Stone Mastic Asphalt |  |
| Combined Binder Course and Base Course | 245mm | 150mm | Dense Macadam (CL 903) |  |
| Sub-base and Backfill | 500mm minimum | 500mm minimum | Type 1 granular sub-base compacted in 100mm layers (CL 803) |  |

Footway or Shared Surface Roads (Permanent Reinstatement)

| Layer | Bituminous Surface | Slabs or Block Paving (c) | Granolithic Surface |  |
| --- | --- | --- | --- | --- |
| Surface Course (b) | 30mm Rolled Asphalt (CL 910) | Relay identical slabs/blocks on 50mm sharp sand (Appendix 11/1) | 40mm of Granolithic Concrete (CL 1704) |  |
| Binder Course | 50mm Dense Macadam (CL 906) |  | 75mm 25/37.5mm Concrete (CL 1704) |  |
| Base Course and Sub-base | 150mm of Type 1 Granular Fill (CL 803) | 175mm of Type 1 Granular Fill (CL 803) | 150mm of Type 1 Granular Fill (CL 803) |  |
| Backfill | Varying thicknesses of Type 1 Granular Fill (CL 803) |  |

- The surface course material shall match the surrounding surface course. Contact the Council for further guidance if required.

- Prior to compaction 10mm limestone chippings shall be applied at a rate of 1kg/m2 to the surface course.

- On shared surface carriageways the block paving reinstatement specification shall apply.

## NOTES:  THE ROADS (SCOTLAND) ACT 1984 SECTION 56 STATES

- No works shall be executed in, or excavation made under, a public road except with the Roads Authority’s consent in writing and in accordance with any reasonable conditions, which they think fit to attach to the consent.

Note:	Persons contravening this section shall be guilty of an offence and shall be liable to a fine not exceeding £200 (December 1985).

- A person shall, as soon as reasonably practicable make good any damage to the road occasioned by the works or excavation and shall immediately thereafter give notice to the authority that the damage is made good; and until twelve months have elapsed from the authority certifying that the damage has been made good to their satisfaction the person shall maintain so much of the road as is made good.

- Works executed, or an excavation made, in contravention of 1 above, made be removed, or as the case may be, filled in by the Roads Authority who may recover such expenses as are reasonably incurred in so doing.

# Commercial Services – Roads

# Road Opening Permit Applications

Please note that Road Opening Permits will not be processed by Commercial Services (Roads) unless the following documents are returned with the completed permit application.

- A copy of your current Public Liability Insurance  Policy

- A copy of your qualifications for working on the public road (i.e. HAUC Supervisors and Operatives Permits or SQA/CITB Highway Maintenance Qualifications).